## Slide 1
CALPHAD: CALculation of PHAse Diagram
Archie Yao

## Slide 2: High Level Idea: What Is CALPHAD?
CALculation of PHAse Diagram based on thermodynamic modeling
Infer the “status” of the system at given composition, temperature & pressure, draw phase diagram accordingly.
Minimizing the free energy of the system:
: the mole fraction of the j-th species in the i-th phase
: the fraction of the i-th phase
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 3: Key Components
Models for Gibbs Free Energy
Core Idea: Minimizing Gibbs Free Energy
Phase Stability & Phase Coexistence
Workflow of CALPHAD
Differentiable CALPHAD
Code Demo (pycalphad + JAX-TherMo)
Exam
Basic Knowledge of Thermodynamics
Computational Thermodynamics
Write these understandings in code
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 4: What Is Phase Diagram?
Phase diagram is consisted of different regions which represent different phases
According to thermodynamics, the “status” (i.e. phase) that the system should be in must minimize the Gibbs free energy of the system：
Different phases have different expressions for Gibbs free energy
Ni-Cu
Na-K
: the mole fraction of the j-th species in the i-th phase
: the fraction of the i-th phase
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 5: First Things First: Gibbs Free Energy of Solution
For all solution phases (i.e. mixture of substances, can be liquid solution / solid solution), the Gibbs energy is given by the general formula:
is the ideal mixing contribution (i.e. assuming no interaction between substances, only the entropy contributes to mixing Gibbs free energy)
is the excess part, usually described by the famous Redlich-Kister polynomial expansion:
is the contribution of pure substance
Coefficients can be looked up at Scientific Group Thermodata Europe database
Notes: SER: standard element reference state
The expression of is valid for both pure species or stoichiometric compounds
So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 6: Second Law of Thermodynamics
Any system working at constant NPT condition tends to have minimum Gibbs free energy
Although, kinetics might prevent this happening (the famous graphite VS diamond case, Atkins)…
G
x(A)
A made-up example: Gibbs free energy of A-B alloy
A-B alloy has two distinct possible structures: fcc & hcp
x represents the mole fraction of A in the alloy. x=0 means the whole alloy is consists of B only, x=1 means the whole alloy is consists of A only.
The Gibbs free energy of these two structures are plotted
In this simple example, since is always lower, the alloy will always in fcc phase instead of hcp phase
ALTHOUGH, kinetics might let you see A-B alloy in hcp structure
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 7: Second Law of Thermodynamics
What about this system?
G
x(C)
But really, are things that simple?
REALLY????
A made-up example: Gibbs free energy of C-D alloy
C-D alloy has two distinct possible structures: fcc & hcp
x represents the mole fraction of C in the alloy. x=0 means the whole alloy is consists of D only, x=1 means the whole alloy is consists of C only.
The Gibbs free energy of these two structures are plotted
Your first guess
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 8: Second Law of Thermodynamics
What about this system?
G
x(C)
But really, are things that simple?
REALLY????
Your first guess
A made-up example: Gibbs free energy of C-D alloy
C-D alloy has two distinct possible structures: fcc & hcp
x represents the mole fraction of C in the alloy. x=0 means the whole alloy is consists of D only, x=1 means the whole alloy is consists of C only.
The Gibbs free energy of these two structures are plotted
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 9: Things Are NOT That Simple... Phase Stability
Consider the Gibbs free energy of a binary mixture of substances A and B
If the system has only one phase when the concentration of substance A is , then Gibbs free energy of the whole system is
What phases will the system decompose into?
Constraint: the Gibbs free energy of the system should be minimized:
Phase Separation!
However, if the system decomposes into mixture of two phases, one having the concentration of substance A of , one having the concentration of substance A of , the system will have a lower Gibbs free energy than having one single phase
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 10: Common Tangent Approach
i.e.
Result does not contain , i.e. this relation holds for any within the range of
Find out and with Newton-Raphson method (learn on Wikipedia if you don’t know it)
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 11: General Common Tangent Approach
Assuming in liquid and solid (i.e. fcc) phases, there is no further phase separation
i.e.
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 12: When Is a Phase Unstable?
Second law of thermodynamics tells us a system at constant NPT tend to have a minimum Gibbs free energy
, unstable!
For a two-component system:
positive definite
Hessian matrix
Stability requires
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 13: Why Stability requires
Second law of thermodynamics tells us a system working at constant NPT tend to have a minimum Gibbs free energy
Consider two systems A & B, both in constant NPT and in equilibrium with each other
Now perturb the system a little bit by moving amount of type 1 particle from B to A. The change of total Gibbs free energy is
Because at first the two systems are in equilibrium (i.e. Gibbs free energy minimized), we must have . And since equilibrium implies(i.e. equal chemical potential), we have> 0. Since A and B are arbitrary system, we must have
for arbitrary system
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 14: Why Equilibrium requires
Second law of thermodynamics tells us a system working at constant NPT tend to have a minimum Gibbs free energy
Consider the Gibbs free energy of a system in NPT condition
Now, we arbitrarily divide the system into 2 parts A & B,
Because the number of the particle in the whole system cannot change, we must have
Because Gibbs free energy is extensive quantity, we have
Second law of thermodynamics tells us any spontaneous process at constant NPT requires minimization of Gibbs free energy
When at equilibrium, we must have
Therefore , i.e. , i.e.
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 15: Workflow of CALPHAD
Core task: looking for thermodynamic equilibrium, i.e. find those points on the phase boundary
Step 1: find the Gibbs free energy model for all possible phases (e.g. bcc, fcc, hcp, liquid etc.) in your system
Step 2 [Optional but highly recommended, for better convergence]: do global minimization of Gibbs free energy with convex hull algorithm to give the initial solution for phase boundary
Step 3: Refine the initial guess with the common tangent approach
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 16: Convex Hull Algorithm
A method of detecting approximate phase boundary, the result from this algorithm will be the initial guess for the common tangent approach
Key idea: if a piece of convex hull is significantly longer than the other pieces, it must be because this piece of convex hull “bridges” over a concave region (i.e. where phase separation happens)
On a set of evenly sampled grid (), the convex hull at convex region will be ultimately consists of lines connecting neighboring sampling points. A long piece of convex hull only appears at the concave region
G
x
Sample points
Convex Hull
G
x
Convex Hull
No phase separation
Phase separation
Sample points
Initial guess for phase boundary
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 17: How Does Convex Hull Work?
G
x
Sample points
Convex Hull
For each piece of convex hull, pick the point with furthest distance outside the whole convex hull and reconstruct two new pieces of convex hull
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 18: Make CALPHAD Differentiable!
Simple realization: write everything in differentiable framework – Jax TherMo by Pinwen
Calculates the sensitivity of result wrt the parameters in the Gibbs free energy models
Update the parameters in the Gibbs free energy models according to loss function
Guan et al, Scripta Materialia (2022)
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 19: Loss Function
Ideal case: , where and are the points on phase equilibrium at temperature T, and are the predictions given by your model in training process.
What if your prediction does not contain these phase coexisting regions?
Driving Force (DF) loss for phase separation that doesn’t appear in the prediction
Hessian loss for miscibility gap that doesn’t appear in the prediction
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 20: Driving Force Loss for Missing Phase Separation
For each metastable phase one can determine the distance in terms of Gibbs energy between the stable tangent plane and a tangent plane parallel to the metastable phase. This distance is regarded as the “driving force”. Most often the driving force is divided by RT and thus rendered dimensionless.
Lucas et al, Computational Thermodynamics: The Calphad Method (2007)
Notes: Lukas, H., Fries, S., & Sundman, B. (2007). Basis. In Computational Thermodynamics: The Calphad Method (pp. 7-46). Cambridge: Cambridge University Press. doi:10.1017/CBO9780511804137.003
So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 21: Hessian Loss for Missing Miscibility Gap
Why the miscibility gap is missing from the prediction?
Miscibility gap indicates instability, i.e. there is a region that .
Missing the miscibility gap means
We should penalize in the loss function if
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 22: Core Take-Away
We want the phase diagram for a given system
I.e. we want to find those points on the phase boundary in the phase diagram
To do this, we first figure out the expression of Gibbs free energy of all possible phases in the system
Then we minimize the Gibbs free energy given any components & temperature
The convex hull algorithm helps locate the concave region of , thus locating the phase coexisting regions (if there is phase coexisting region. If the landscape of G is like the one in slide 6, then no phase coexisting regions)
Common tangent algorithm gives the accurate phase boundary according to the initial guess given by convex hull
If you write all the things above in a differentiable framework, you get differentiable CALPHAD
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 23: EXAM: Thermodynamics of Cm-U Alloy
Scientists have just identified a new alloy, i.e. the Cm-U alloy. The Cm-U alloy has two possible phases: cit phase and scs phase. The expression of Gibbs free energy for the two phases are:
At , plot and VS . What phase is the Cm-U alloy in?
Draw the chemical potential of cit and scs phase at .
If there is a two-phase region at , use the common tangent approach to give the range of two-phase region and specify what are the two phases. If there is no such region, explain why.
At , plot and VS . Define , plot on the same figure where you plot and .
Is there phase separation at ? If there is, find out the range (hint: Newton-Raphson method). If there is not, explain why.
where is the mole fraction of , is the temperature,
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)

## Slide 24: Code Demo: pycalphad & Jax-TherMo
Notes: So how do we get 𝐑_0+∫1▒𝐕d𝑡 at arbitrary time step 𝑡? One possible solution is to save 𝐕 at every intermediate checkpoint of NODE, and delete the value of 𝐕 at the previous checkpoint when reaching the new checkpoint (might need some slight modifications of NODE packages in order to save the checkpoints)